## Slide 1
Seismic category C1 tests simulate earthquake load cycling in 0.5mm stationary cracks
Hard tests but milder than those of required for seismic category C2. Can be seen as an “entry level” seismic qualification.
Pulsating tension tests
Alternating shear tests
Dw= 0.5mm
C1
Note: for static approval crack width 0.3mm
Note: Cracked concrete relevant tests are conducted before qualifying anchor according to seismic C1 or C2

## Slide 2
Seismic category C2 tests simulate earthquake load cycling in 0.8mm dynamic cracks
Pulsating tension tests
Alternating shear tests
Open/closing crack width
Dw= 0.8mm
Dw = 0 – 0.8mm
C2
Note: for static approval crack width 0.3mm
Cyclic load
With enforced compressing force to close crack
N
t
Load increasing along with crack cycling range increasing
Displacement during load/crack cycling is less than 7mm
After load/crack cycling, capacity of fastening system can still reach 90% static resistance
Resistance scatter is within the limit as static